## Slide 1: Digital Image Correlation
Egil Fagerholt
25 August 2015

## Slide 2
Reference image
No deformation
Current image
At deformed stage
Disp. Y
Disp. X
Strain
Load cell
Linear transducer
DIC – Basic Principle
Example: Uniaxial tension test
DIC
Random speckle pattern
Camera
Optical axis normal to specimen surface (2D-DIC)

## Slide 3
DIC – 2D vs. 3D setup
3D
Two cameras
Stereovision
2D
Single camera
Target
coordinates
Requirements:
Optical axis normal to
specimen surface
Specimen surface is plane
during experiment
Limitations:
Only in-plane displacements
are measured
Benefits:
Simple setup
Limited camera calibration
Requirements:
Full camera calibration
Benefits:
Specimen may have an
arbitrary shape
Both in-plane and out-of-plane
displacements are measured
General limitations (both 2D and 3D): No through-thickness deformation is measured

## Slide 4
DIC versus traditional measurement techniques
Extensometer
Strain gauges
Elongation over a
fixed distance
Strain in a small area
2D-DIC
Full-field displacement/strain measurements
Elongations extracted during
post-processing
3D-DIC
Laser
Deflection of plate

## Slide 5
DIC – Measurement uncertainty
Measurement uncertainties are mainly due to grayscale noise in the recorded images,
which varies from camera to camera.
Typical resolution in displacements are less than: 0.1 pixel
5MP (2448 x 2050 pixels)
Specimen length: 200 mm
Specimen width: 12.5 mm
Example: Uniaxial tension test
Strain resolution is typically down to
Local strains as high as 200% can be measured (e.g. polymers)

## Slide 6
DIC - Measurement uncertainty
Large elements -> Less suceptible to grayscale noise
Small elements -> better description of disp. field
Compromize

## Slide 7: Software eCorr
Graphical Interface
DIC Core
Main Functionalities
Recording of image series
Camera calibration for 3D-DIC
Mesh generation/modification
2D/3D-DIC Analysis
Visualization and export of data

## Slide 8: Range of applications Examples
Material tests
Crack propagation
Point Tracking
Pipeline Impact
Component Tests
Blast loading of plates

## Slide 9: Material model validation DIC-FEM coupling
Strains measured by DIC
Calculated stress fields
Material
model
Material model parameters
Cross section
Computed force
from DIC and material
model
Experimental force
from load cell

## Slide 10: Validation of 3D-DIC SIMLab Shocktube

## Slide 11: Validation of 3D-DIC Camera Calibration

## Slide 12: Validation of 3D-DIC Initial Results
Aluminium
0.8 mm
2.5 bar
Avvik ~ 1/100 mm
Steel
0.8mm
75 bar

## Slide 13: Validation of 3D-DIC Frame tracking
Steel
0.8mm
40 bar

## Slide 14: Validation of 3D-DIC

## Slide 15
Validation of 3D-DIC