## Slide 1: Digital Image Correlation (DIC)
Egil Fagerholt

## Slide 2
Reference image
No deformation
Current image
At deformed stage
Disp. Y
Disp. X
Strain
Load cell
Linear transducer
DIC – Basic Principle
Example: Uniaxial tension test
DIC
Random speckle pattern
Camera
Optical axis normal to specimen surface (2D-DIC)

## Slide 3
DIC – Tracking of grayscale pattern

## Slide 4
DIC – Material point tracking (Subset-based formulation)
[4] Sutton MA, McNeill SR, Helm JD, Chao YJ (2000) Advances in two-dimensional and three-dimensional computer vision
Current image
Deformation parameters (linear subset):
Function to minimize (SSD):
Reference configuration position vector:
Displacement vector:
Current configuration position vector:
Reference image
Subset

## Slide 5
DIC – Global «finite element» formulation
[5] Besnard G, Hild F, Roux S (2006) “Finie-element” displacement fields analysis from digital images: application to Portevin-Le Chatelier bands
”Stiffness matrix”
Weighted sum of grayscale
gradients.
”Load vector”
Weighted sum of grayscale
differences and gradients.
Nodal degrees of freedom increment
Iterated until a correlation criteria is fulfilled
Function to minimize (SSD):
Decomposing to finite elements
Global equation
Assembly of element contributions

## Slide 6
DIC versus traditional measurement techniques
Extensometer
Strain gauges
Elongation over a
fixed distance
Strain in a small area
DIC
Displacement and strain fields are measured
over the specimen as viewed by the camera
Elongations can be extracted during
post-processing

## Slide 7
DIC – Measurement uncertainty
Measurement uncertainties are mainly due to grayscale noise in the recorded images,
which varies from camera to camera.
Typical resolution in displacements are less than: 0.1 pixel
5MP (2448 x 2050 pixels)
Specimen length: 200 mm
Specimen width: 12.5 mm
Example: Uniaxial tension test
Strain resolution is typically down to
Local strains as high as 200% can be measured (e.g. polymers)

## Slide 8
DIC - Measurement uncertainty
Large elements -> Less suceptible to grayscale noise
Small elements -> better description of disp. field
Compromize

## Slide 9
- Examples (Docol 600DL)
Strain fields from 2D-DIC
Uniaxial tension
Plane strain
Arcan-45

## Slide 10
DIC – 2D vs. 3D setup
3D
Two cameras
Stereovision
2D
Single camera
Target
coordinates
Requirements:
Optical axis normal to
specimen surface
Specimen surface is plane
during experiment
Limitations:
Only in-plane displacements
are measured
Benefits:
Simple setup
Limited camera calibration
Requirements:
Full camera calibration
Benefits:
Specimen may have an
arbitrary shape
Both in-plane and out-of-plane
displacements are measured
General limitations (both 2D and 3D): No through-thickness deformation is measured

## Slide 11
DIC Software
Record image series
from GigaEthernet cameras
Mesh generation and
analysis preparation
Run analyses
2D- or 3D-DIC
Camera calibration
Study and export results
(displacements and strains)
Graphical user interface (GUI)
Data filtering and coupling with
material models

## Slide 12
DIC – Strain calculations
Assume no
out-of-plane deformation
Assume no shear strain
through thickness
Deformation gradient
Green deformation
Principal streches (eigenvalues of C)
Principal strain components
Assume negligible elastic strains
and plastic incompressibility
Effective strain based on von Mises norm
2D-DIC
Displacement gradient

## Slide 13
DIC Software – Meshing
Structured mesh
Meshing is done in DIC software GUI
Non-structured mesh
Manually define boundries of specimen
Generate Python script for Abaqus
Use Abaqus meshing tool to generate mesh
Import Abaqus «input-file» in DIC software

## Slide 14
Selected element
Selected vector
Vector elongation
Principal strain components
Strains through cross section
DIC Software – Data Visualization

## Slide 15
Element erosion
A discontinuous displcement field is captured
No data lost (eroded)
An initial analysis has to be carried out
Node splitting
DIC Software – Handling propagating cracks

## Slide 16
DIC Software – Node splitting

## Slide 17
DIC Software – 3D-DIC - Camera calibration
Camera 1
Image coordinates
[pixels]
Camera 2
Image coordinates
[pixels]
Target coordinates
[mm]
Camera model
Camera 1
Camera model
Camera 2
Multiple calibration targets may be used to increase accuracy of camera models

## Slide 18
- Uniaxial circular specimen (PVC)
3D-DIC
Specimen cross section

## Slide 19
- Bulge test
3D-DIC
Out-of-plane displacement profiles
3D model with strain field
Camera 1
Camera 2

## Slide 20
- Compression of aluminium profiles
3D-DIC
3D model

## Slide 21
- Blast loading of aluminium plates (high-speed cameras)
3D-DIC
Out-of-plane displacement [mm]

## Slide 22
Thank you for listening!